Pag. 1 of 2

WHITE 800

Technical Data Sheet                                  Rev. 13/07/2011

1. Особенности

Белая полиуретановая полуматовая эмаль

· хорошее заполнение

· тиксотропность

·  высокая твёрдость

· отличная химстойкость

2.Химические и физические особенности

2.1 Химическое описание         Смесь алкидных смол

2.2 Цвет                                    Белый

2.3 Вязкость                              2’15’’± 10’’ (CF4 at 20°C)

2.4 Сухой остаток                      55% ± 0.5%

2.4 срок годности                     12 месяцев

2.5 Условия использования       18 до 35°C

3.Приготовление продукта

3.1 Продукт                         WHITE 800                      100%

3.2 Катализатор                  0815 M 240                       50%

3.3 Разбавитель                  0391 THINNER 214       30-40%

3.3 Время жизни смеси    > 4 часа при 20-25°C

4.Настройки:

4.1 Основание              Предварительно загрунтованные панели

All IVE products are for professional use; this means that the operator should have a good knowledge about the right usage of the

products especially in relation with technical and safety matters.

All the information in this technical data sheet are based on IVE best know-how, experiences and lab test. These information have to be

intended for general usage of the products; as IVE cannot control each single customer we decline any responsibility about an incorrect

usage of the products or their usage in not-standard sequences.

IVE assure that its products complies in the time to the original chemical-physical standards.

IVE Coatings S.r.l. – Via Toscanini, 53 – 20038 Seregno (MB) – Tel. +39 0362 231401 – E-mail mail@ive.it

Pag. 2 of 2

WHITE 800

Technical Data Sheet                                  Rev. 13/07/2011

5.Время сушки:

5.1 от пыли                       около 30 минут

5.2 на отлип                      около 60 минут

5.3 Штабелирование         6 часов

5.4 Полное высыхание      7 дней

5.5 Быстрая сушка            60 минут при 35-40°C

6.Процесс нанесения:

All IVE products are for professional use; this means that the operator should have a good knowledge about the right usage of the

products especially in relation with technical and safety matters.

All the information in this technical data sheet are based on IVE best know-how, experiences and lab test. These information have to be

intended for general usage of the products; as IVE cannot control each single customer we decline any responsibility about an incorrect

usage of the products or their usage in not-standard sequences.

IVE assure that its products complies in the time to the original chemical-physical standards.

IVE Coatings S.r.l. – Via Toscanini, 53 – 20038 Seregno (MB) – Tel. +39 0362 231401 – E-mail mail@ive.it

# Text boxes

|  | Низкое давление |
| --- | --- |
| давление | 4 bar |
| дюза | 1.6 мм |
| вязкость | 14’’-16’’ CF4 |
| расход | 100 - 180 г/м2 |

| шаг | количество | Время сушки |
| --- | --- | --- |
| Шлифовка 120-150-180 | // | // |
| Грунтование | 300 г/м2 | 12 часов |
| шлифовка 320-400 | // | // |
| WHITE 800 | 150 г/м2 | 12 часов |